pRODUCT 1104133 –1 PLY BLUE C’FOLD TOWEL

SPECIFICATION

| Characteristics | Units | Specifications |
| --- | --- | --- |
|  |  | Target | Min | Max |
| Total Grammage | g/m2 | 36.0 | 36.6 | 35..4 |
| Colour | Blue |  |  |  |
| Raw Material | Recycled |  |  |  |
| Brightness | % | N/A |  |  |
| Sheet Width | mm | 217 | 212 | 222 |
| Sheet Length | mm | 250 | 246 | 254 |
| Sleeves per Case | 12 |  |  |  |
| Sheets per Sleeve | 240 |  |  |  |
| Sheets per Case | 2,880 |  |  |  |
| Cases per Pallet | 10 0 |  |  |  |

09/10/23

ISSUE 1